SUSTAINABLE BIOPLASTIC PRODUCED PROM agricultUrAL waste: A SOLUTION FOR REDUCING PLASTIC POLLUTION

Hong T. Pham 1,* Cuong Nguyen Chi1, Nguyen Nguyen Thi The1, Anh Pham Nguyet1, Lien Nguyen Thi1, Linh Hoang Bao1, Khuong V. Dinh2,3

(1) Department of Environmental Engineering, Chemistry and Environment faculty, Thuyloi University, 175 Tay Son street, Dong Da, Ha noi

(2) Department of Fisheries Biology, Nha Trang University, No 2 Nguyen Dinh Chieu Street, Nha Trang City, Vietnam, email: Khuong.dinh@ntu.edu.vn

(3) National Institute of Aquatic Resources, Technical University of Denmark, Lyngby, Denmark

*Email: hongpt@tlu.edu.vn

Received date:

Published date:

# Abstract.

# Plastic pollution is a global issue, seriously affecting soil by preventing oxygen intake, causing soil erosion and degradation. The outbreak of COVID-19 has worsened the plastic pollution from traditional plastic face masks. Million tons of agricultural garbage mainly rice straw and sugarcane garbage were produced in Asian region causing difficulties in treatment. Most of them was burned at field releasing small particle PM 2.5 and air pollutants. The goal of this paper is transforming a cellulose material wastes, particularly rice straws and sugarcane bagasse into bio-plastic products that can replace traditional degradable plastics. Several steps were conducted to extract the maximum mass of cellulose from agriculture residue. To minimize the chemical use, a new approach in the repreparation steps was conducted by integrating enzymes in extracting cellulose. Different ratios of adding chemicals and processes were applied to form and mold plastic film. The new bioplastic materials generated from rice straw and sugarcane garbage exhibit a good mechanical property with tensile strength from 10 to 42 MPa. The elongation was from 25% to 100% in different ratios of plasticizers and types of cellulose material. The morphology of bio-plastic was investigated by scanning electron microscopy (SEM) showed a uniform and compact structure. The changing functional groups were analyzed by infrared spectrum IR. 2D-Xray analysis showed bioplastic is amorphous. The half-life of these bioplastics were 20 days under the landfill condition. The results showed that different methods of extraction and molding will produce bio-plastic with different properties. Bioplastic from agricultural waste is a high potential plastic for various applications. This result will help reduce traditional plastic pollution and CO2 emissions to the atmosphere by burning agriculture residue, thereby contributing to the Sustainable Development Goals of The United Nations.

Keywords: Bio-plastic, agriculture waste, plastic pollution, cellulose material, CO2 footprint

Classification numbers: 3.4.1. 3.3.1, 3.3.3